## Slide 1
First pass with 209 wafers
Got 46 clusters
Largest cluster has 148 wafers
  66 have up to 1 DBC per chip
  82 have no DBC at all
Because we have wafers with up to 70 DBC on a single chip, a lot of the 1 DBC per chip wafers are clustered with the 0 DBC
If I decrease the t values from 5 to 2, I can get a largest cluster with 88 wafers where almost all of them have no DBC at all

## Slide 2
First pass with 209 wafers
Got 46 clusters
45 of the 46 clusters contain 61 wafers with CANOP
Some of these wafers with similar largest fail counts on the same chip are grouped together
Observation: Fail magnitude plays a very large role in the clustering

## Slide 3
Using DBC yield instead of count
Forcing 2 clusters
  Cluster 0 with 195 wafers
  Cluster 1 with 14 wafers
Smaller cluster has wafers with largest area taken by DBC fails

## Slide 4
Using DBC yield instead of count
Forcing 5 clusters
  Cluster 0 with 167 wafers
  Cluster 1 with 28 wafers
  Cluster 2 with 2 wafers
  Cluster 3 with 11 wafers
  Cluster 4 with 1 wafer
Cluster 1
Cluster 2
Cluster 3
Cluster 4

## Slide 5
I had to force 98 clusters to get a group with only the non CANOP wafers
  Cluster 0: 82 wafers (Only non CANOP wafers)
  Cluster 1: 8 wafers
  Cluster 2: 8 wafers
  Cluster 3: 4 wafers
  Cluster 4: 4 wafers
Cluster 1
Cluster 2
Cluster 3
Cluster 4